|  | SLEWING RING INSPECTION REPORT |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Type: RB12025UUCCO-P5 |  |  | Size:Φ180xΦ120x25 |  |  |  |  |  |
| Date of checking :2010-4-24 |  |  | Lot Quality : 1 |  |  |  |  |  |
| Project |  | Standard | Measuring Method | Detection Record |  |  |  |  |
|  |  |  |  | 01 |  |  |  |  |
| Material |  | GCr15 | Material Report | GCr15 |  |  |  |  |
| Appearance |  | No bruising, Nick | Visual | No |  |  |  |  |
| Outer Diameter |  | Φ180-0.025 | External Micrometer | -0.01 |  |  |  |  |
| Inner Diameter |  | Φ120-0.02 | Internal Micrometer | -0.01 |  |  |  |  |
| Total Height |  | 25-0.10 | Micrometer | -0.05 |  |  |  |  |
| Outer Height |  |  | Micrometer |  |  |  |  |  |
| Inner Height |  | 25-0.075 | Micrometer | -0.025 |  |  |  |  |
| Outer Parallel Tolerance |  | ≤0.008 | Dial Gauge | 0.006 |  |  |  |  |
| Inner Parallel Tolerance |  | ≤0.007 | Dial Gauge | 0.005 |  |  |  |  |
| Inner Facing Bounce |  | ≤0.010 | Dial Gauge | 0.008 |  |  |  |  |
| Inner Radial Bounce |  | ≤0.010 | Dial Gauge | 0.007 |  |  |  |  |
| Inner Ellipse |  | ≤0.011 | Dial Gauge | 0.009 |  |  |  |  |
| Inner Taper |  | ≤0.008 | Dial Gauge | 0.005 |  |  |  |  |
| Axial Clearance |  |  |  |  |  |  |  |  |
| Radial Internal Clearance |  | -0.01～0 | Dialgauge | 0 |  |  |  |  |
| Outer Connection Hole |  | 6-Φ3.2 Uniform Distribution,Counter Bore6-Φ6Deep 3.5 | Slide Caliper | Qualify |  |  |  |  |
| Orifice Rounding Chamfer |  | Yes | Visual | Qualify |  |  |  |  |
| Threaded Hole Burr |  |  | Visual and Touch | No |  |  |  |  |
| Oil Hole Specifications |  | 3-Φ3.5 | Internal Screw Gauge Slide Caliper | 3 |  |  |  |  |
| Bearing Hardness |  | 58-62HRC | HRC | 60HRC |  |  |  |  |
| The oil sealed |  | Yes | Visual | Yes |  |  |  |  |
| Seal Joint |  | Adhesive Bonding | Visual and Touch | Qualify |  |  |  |  |
| Roughness of the seal of overlapped labial |  | Bellow Ra3.2 | Visual | Qualify |  |  |  |  |

Conclusion:Qualify                                                                      Inspector: Gao Yunpeng